## FIELD OF APPLICATION

This technical specification is valid for all casted strips from aluminium and its alloys by horizontal twin roll casters. 95% of all inspected values have to be within tolerances in this document and will be evaluated at steady state flow conditions.

## DISPATCH, DELIVERY, MATERIAL IDENTIFICATION

Each strip is identified by:

The ID of the strip (8-12 symbols)

The weight of the strip

The thickness of the strip

The width of the strip (after edge milling/trimming)

The alloy

The date of production

Production time (from start-up/cutting beginning to the end of the coiled strip)

Number of the batch

Number/Letter of the casting line

Data Matrix (DTM)

## TECHNICAL DEMANDS

### Chemical composition

The target chemical composition of the alloys will be according to Tab. 1 to Tab. 7. It will also be possible to cast alloys: 1050, 3003, 3005, 8006, 8011 and 8079 with the chemical composition specified in the EN 573-3 standard. The casting equipment will also allow the casting of hard alloys such as: 5052 and 5754. Chemical composition will be evaluated based on OES measurements.

Table 1 Chemical composition of alloy 1050

| Cu: | max. 0.02 % | Si: | max. 0.2 % | Zn: | max. 0.05 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.01 % | Fe: | max. 0.3 % |  |  |
| Mn: | max. 0.03 % | Ti: | max. 0.05 % |  |  |

Min. Al:			99.5 %

Other individually:		0.03 %

Other in total:			0.5 %

Table 2 Chemical composition of alloy 3003 (Zn)

| Cu: | 0.1 – 0.2 % | Si: | 0.5 – 0.6 % | Zn: | max. 1.4 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.02 % | Fe: | 0.45 – 0.55 % |  |  |
| Mn: | 1.0 – 1.1 % | Ti: | max. 0.05 % |  |  |

Min. Al:			The rest

Other individually:		0.05 %

Other in total:			0.15 %

Table 3 Chemical composition of alloy 3003 (Zr) - ZIRKAL

| Cu: | max. 0.05 % | Si: | 0.5 – 0.6 % | Zn: | 0.9 – 1.6 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.02 % | Fe: | max. 0.25 % | Zr: | 0.1 – 0.15 % |
| Mn: | 1.1 – 1.2 % | Ti: | max. 0.05 % | Cr: | 0.1 – 0.2 % |

Min. Al:			The rest

Other individually:		0.05 %

Other in total:			0.15 %

Table 4 Chemical composition of alloy 3005 - PROFAL

| Cu: | max. 0.3 % | Si: | max. 0.15 % | Zn: | max. 0.25 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | 0.2 – 0.6 % | Fe: | 0.45 – 0.55 % |  |  |
| Mn: | 1.0 – 1.3 % | Ti: | max. 0.05 % |  |  |

Min. Al:			The rest

Other individually:		0.05 %

Other in total:			0.15 %

Table 5 Chemical composition of alloy 8011

| Cu: | max. 0.05 % | Si: | 0.55 – 0.65 % | Zn: | max. 0.05 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.01 % | Fe: | 0.55 – 0.69 % |  |  |
| Mn: | max. 0.02 % | Ti: | max. 0.05 % |  |  |

Min. Al:			The rest

Other individually:		0.05 %

Other in total:			0.15 %

Table 6 Chemical composition of alloy 8079

| Cu: | max. 0.02 % | Si: | 0.05 – 0.15 % | Zn: | max. 0.1 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.02 % | Fe: | 1.00 – 1.15 % |  |  |
| Mn: | max. 0.02 % | Ti: | max. 0.05 % |  |  |

Min. Al:			The rest

Other individually:		0.05 %

Other in total:			0.15 %

Table 7 Chemical composition of alloy 8006

| Cu: | max. 0.05 % | Si: | max. 0.2 % | Zn: | max. 0.05 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | max. 0.005 % | Fe: | 1.27 – 1.40 % |  |  |
| Mn: | 0.35 – 0.42 % | Ti: | max. 0.05 % |  |  |

Table 8 Chemical composition of alloy 5052

| Cu: | 0.1 % | Si: | >0.25 % | Zn: | >0.1 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | 2.2-2.8 % | Fe: | >0.35 % |  |  |
| Mn: | 0.1 % | Ti: | >0.15 % |  |  |

Table 9 Chemical composition of alloy 5754

| Cu: | >0.1 % | Si: | >0.35% | Zn: | >0.2 % |
| --- | --- | --- | --- | --- | --- |
| Mg: | 2.6-3.6% | Fe: | >0.35 % |  |  |
| Mn: | >0.5 % | Ti: | >0.15 % |  |  |

Min. Al:			The rest

Other individually:		0.02 %

Other in total:			0.15 %

### Metal quality

The reduction of hydrogen content will be measured by an appropriate Hydrogen analyser instrument designed for the evaluation of hydrogen content in Al melt such as AlSCAN or other corresponding technique at steady state flow. Inclusions reduction will be measured at steady state flow conditions via mobile liquid aluminium cleanliness analyzer (LiMCA) and/or on Alcan PoDFA technique.

Degasser requirements:

Efficiency of Hydrogen removal shall be minimum of 75 %. With a target post degasser value of 0.13 cm3/100 g Al.

Unit shall demonstrate an inclusion removal rate of 30-35 % of the incoming and outgoing metal stream at steady state flow

Unit shall demonstrate removal of 50 – 70 % of Na & Ca at stoichiometric chlorine input based on OES measurements of incoming vs. outgoing metal stream at steady state flow. Li removal to be determined & agreed by Contractor and customer

Similar requirements for Na & Ca are required if Salt is utilized instead of Chlorine

Table 8 Degasser requirements for Hydrogen and Inclusions removal.

Filter requirements:

98 % reduction in 20 µm inclusions at steady state flow conditions measured before and after filter.

85 % reduction in 10 µm inclusions at steady state flow conditions measured before and after filter.

Metal cleanliness:

An average PoDFA post filter during steady state casting to the casting center with a PoDFA count of less than 0.05 mm2/kg—Titanium Borides included.

An average PoDFA post filter during steady state casting to the casting center with a PoDFA count of less than 0.002 mm2/kg—Titanium Borides excluded.

### Strip internal structure

The internal structure of the strip will be checked on polished samples using optical microscopy. Techniques such as HF (hydrofluoric acid) etching to reveal intermetallic phases, or HBF4 (Fluoroboric acid) etching for grain structure analysis under polarized light will be used. If the relevant norm is not specified, the measurement of the relevant lengths will be carried out using measuring lines within the software of the relevant optical microscope. The average grain size will be evaluated in accordance with ASTM E112-10:2010.

Generally, an equiaxed grain structure of as cast strip is required. Illustrative picture of differences between equiaxed and prolonged grain structure is shown in Fig. 1

a) Equiaxed grain structure		b) Prolonged grain structure

Fig. 1 Example of a) equiaxed grain structure and b) prolonged grain structure with columnar grains – illustrative photos.

Average grain size by ASTM E112-10:2010: G: ≥ 2.5 which corresponds to size of max. 150 µm. Definition is valid for alloys with at least 1 % and more of alloying elements

Grain size in central zone will not exceed max. of 130 µm. Central zone is defined by size of 1/3 of as cast thickness of the strip. Prolonged (columnar like) grains in the surface zone are allowed. The longest side of prolonged (columnar) grain will not exceed max. of 180 µm. Size of the surface zone is defined as 1/3 of as cast thickness of the strip each side (for example: for as cast strip thickness of 6.0 mm, allowed depth of the surface zone is max of 2.0 mm on each side). Definition is valid for alloys with at least 1 % and more of alloying elements

Cracks and pores are not allowed. By the norm ISO 10049:2019, acceptable severity level is 0

Max. allowed size of centreline segregation is 1 % on height of nominal strip thickness. Centreline segregation must be positioned inside the central zone. Size of the central zone is defined as 1/3 of as cast thickness of the strip. Definition is not valid for alloy 8079 at maximum productivity (according to Tab. 9.).

Max allowed size of single (solid) intermetallic particle / phase shall not exceed 5 µm. Example is shown in (Fig. 2). Definition is valid for alloys: 8011 and 8079

Fig. 2 Example of not allowed single (solid) intermetallic particle / phase with size bigger than 10 µm (marked by red arrow).

In case of reduction of casting productivity by 20 % according to data provided in Tab. 9., centreline segregation will not be present in microstructure. Illustrative example of microstructure with and without centreline segregation is show in (Fig. 3). Definition is valid for alloys: 8011, 8079 and 8006.

a) microstructure with centreline segregation

b) microstructure without centreline segregation

Fig. 3 Illustrative example of microstructure with and without centreline segregation in as cast strip.

### Productivity

The required casting productivity according to product mix is as follows:

Table 9 Casting productivity.

As per definition Annex_13_TD_Product mix calculation need to be filled

### Surface quality

Surface quality parameters will be evaluated by visual inspection. Examples of not allowed defects are shown in chapter 8: Definition and examples of defects. Edge burr after edge trimming/milling operation will be evaluated via Vernier with tolerance of 0,001 mm or by optical microscopy measurement on metallographically prepared sample in polished condition.

Upper and bottom cast side:

A uniform, clean and shiny Al surface on the top and the bottom side of the cast strip. Surface defects are not allowed. Change in amount of releasing agent will be adjustable via software to control overlaps and prevent unsprayed areas.

Releasing agent:			max. 250 mg/m2 (graphite solution)

Strip roughness (Ra):			≤ 2 µm

Strip roughness (Rz):			≤ 15 µm

Note: Roughness measurement mode: Cut-off length λc: 0.8; min. evaluation length lm: 12.5 mm, measured in transverse direction to casting.

Edge cutting:

Trimmed or milled edges. After treatment, edges are smooth, clean and free from burrs, nicks, cracks, whiskers or any metal sliver/powder deposited on the surfaces (air blowing is included) from the edge trimming/milling operation. Chips from edge trimmer/miller will be automatically stashed in to boxes in dry conditions.

Width tolerance:			+/- 3.0 mm

Edge burr:				max. 0.3 mm

### Dimensional tolerances

Strip width will be measured by calibrated retractable tape measure or on inspection table using suitable Vernier with tolerance of 0,1 mm.  Strip width will be measured from tension-controlled part of coil. Threading and tale out parts are excluded. Strip as-cast thickness, nominal thickness tolerance, longitudinal strip gauge variation or edges gauge difference will be measured as % deviation of strip thickness by Vernier with tolerance of 0,001 mm or X-Ray. Edge cracks (before edge trimming/milling operation) will be measured by calibrated retractable tape measure. The dimensional tolerances are specified in the EN 485-4 standard.

Nominal thickness tolerance:		max. ± 4%

Range of as-cast thicknesses:		4 to 8 mm

Cast width:				1400 mm

min. 1000 mm

Width tolerance:			± 5 mm (before edge cutting)

Longitudinal strip gauge variation: 	max. 1%

Edges gauge difference:		max. 0.35 % (before edge cutting)

Edge cracks (on cast strip): 		max. 10 mm +/- 1 mm on side

Table 10 Required Crown in transverse direction to casting.

| Nom. thickness (mm) | Crown transverse (%) |
| --- | --- |
| 8 | 0,5 |
| 7 | 0,5 |
| 6 | 0,5 |
| 5 | 0,8 |
| 4 | 1 |

The Crown must be positive and symmetric comparing to nominal thickness (convex lens shape), a negative profile is not allowed. Crown will be measured by the X-Ray gauge meter directly in casting line. If is not possible to measure Crown by X-Ray, measurement by Vernier with tolerance of 0,001 mm must be provided on sample according Fig. 4.

Fig. 4 Schematic of sampling in transverse direction for crown measurement.

### Casting stability

The casting line will be able to cast continuously without interruption (on one tip / nozzle) in campaigns with a minimum total strips weight of at least 500 tons. Casting defects or generally deteriorated quality of the cast strip are not allowed during the whole campaign.

Technological scrap on beginning of casting strip1:			max. 2 000 kg

Time between stop casting2 and ready for new start of a cast3		max. 2 hours

Caster roll exchange time4:						max. 2 hours

Definition:

1-technological scrap is amount of material lost as liquid metal which comes from launder system and coil during the starting until stable casting conditions.

2- stop casting is counted from finish liquid metal from tip to caster roll.

3- ready for the new start of cast means equipment is ready receive liquid metal from holding furnace

- 4- Exchange of complete roll set (upper/lower rolls) shall not take longer than 120 minutes. This value must be warrantied by the Contractor.

### Definition and examples of defects

Not allowed:

Thick skin on melt: Observed in launders, heavily oxidated surface

Excessive cluster / agglomeration: Observed in launders on the bottom, observed by excessive filter or launder system clogging. Also observed in the micro-structure in casted strip as released clusters / agglomeration most often on the bottom side. Very often caused by the grain refiner

Entrapped bubbles: Observed in the casting nozzle (tip) after the end of casting, causes longitudinal lines, or lack of material (thinning)

Blisters: Observed after subsequent rolling process, due to excessive H2 concentration in metal

Surface cracks / microcracks: Observed on the as cast sheet, very often caused by the imprint of the rolls. Thermal fatigue of the rolls (low lifetime of the shells) or by not proper grinding of the rolls

Hot cracks: Observed predominantly at the bottom of the cast surface (when bending the material, cracks open). Cause: casting parameters or setting of the casting nozzle is not optimal. Causes cracks during subsequent rolling operation.

Longitudinal holes: Observed on the as cast sheet, holes accompanied with extra piece of aluminium (presolidification). Cause: casting parameters are not optimal

Rough segregation: Observed in the micro-structure in casted strip. Cause: temperature or casting speed is too high, low cooling capacity of continuous caster

Single (solid) phases / particles: Observed in the micro-structure in casted strip as single intermetallic phase. Particle hardness is usually between HV 100-600

Snake skin: Observed on the as cast sheet and roll surface especially during start-up. Not allowed during production strip casting

Microcracks due to surface segregation: Metal cracks aligned transverse to casting direction. Severe surface segregations

Transversal lines: Observed on as cast sheet, straight transverse lines are often very close together

Level-lines visible in unetched condition: Transversal directed marks observed at as cast sheet. Etching reveal defect. Generally given by casting parameters (fluctuation of meniscus, its magnitude changes with casting temperature, alloy content and tip position)

Lines: Observed on as cast sheet in casting direction

Bleed-out: Observed on as cast sheet. Holes in longitudinal direction. Cause: casting parameters are not optimal or local blockage at tip exit

Black stains: Observed on as cast sheet. Black stains on the strip with increased carbon level in the defect zone. Possible cause: No proper releasing agent layer

Feather structure: Observed in the microstructure, or at strip surface. Large feathery grains. Cause: high temperature, not proper amount of grain refiner.

Visual examples of defects:

Thick skin on melt				Grain refiner clusters

Entrapped bubbles in casting nozzle		Lack of material (thinning)

Blister (excessive H2 concentration)		Blister (after subsequent rolling)

Cracks / microcracks on the sheet surface	Hot cracks

Longitudinal holes (presolidification)		Rough segregation

Snake skin					Single (solid) phases / particles (marked by yellow)

Surface segregation				Surface segregation (micro-structure)

Transversal lines				Levellines

Lines (surface)					Hot lines followed by crack (cross section)

Bleed-out					Black stains

Feather grains (microstructure) 			Feather grains (on the strip surface)